## Slide 1: ME EN 6960: Experimental Methods in Solid Mechanics
Dynamic Fracture
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
References:
Dynamic Fracture Mechanics, L.B. Freund, Cambridge Press 1990
Experimental Techniques in Fracture, J.S. Epstein, SEM 1993
Fracture Mechanics, T.L. Anderson, CRC Press, NY 1994
Handbook on Experimental Mechanics, Kobayashi, SEM 1987
Dynamic Behavior of Materials, M.A. Meyers, Wiley, 1994

## Slide 2
2
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
Measurement of dynamic initiation fracture toughness
Goals:
1) Evaluate the rate dependence of mode I dynamic initiation fracture toughness ()
2) Construct the mixed mode fracture toughness locus for a given rate
3) Study the crack kinking angle as a function of mode mixity and determine the applicability of the maximum hoop stress criterion for crack initiation
In this experiment we will measure the dynamic crack initiation of PMMA; a brittle polymer at room temperature. The goal is to assess both the rate and mode mixity dependence of the material’s fracture toughness. Mode mixity will be introduced using a pre-cracked Brazil disc specimen geometry in diametral compression. Dynamic values of will be obtained using a SPHB for different projectile impact velocities. Quasi-static values of will be determined from provided data on the course website. Because a load-drop indicative of fracture may not be easily identifiable in they dynamic data, a conductive paint gauge and electrical circuit will be used to measure crack initiation.
Once the rate sensitivity of has been established, the dependence of dynamic fracture toughness on mode mixity will be evaluated. Mixed mode dynamic experiments will be conducted by inclining the Brazil disk in the SHPB so that the crack is at an angle to the diametral loading. This will allow variation of mixity from pure mode I to almost pure mode II. In the same fashion as before (i.e., using the static results), and will be measured as a function of mode mixity for one particular rate. Having extracted the values of fracture toughness, the maximum opening (hoop) stress criterion can be used to calculate the predicted angle of crack initiation. The analytical results can be then compared to the experimentally observed kinking angles.

## Slide 3
3
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
Brazil disk fracture specimen:
Nominal specimen dimensions:
and
For values of
consult Atkinson et al, 1982;
Shetty et al, 1987
Conductive Ag paint

## Slide 4
4
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
References:
• Atkinson, C., R. E. Smelser, and Jo Sanchez. "Combined mode fracture via the cracked Brazilian disk test." International Journal of Fracture 18.4 (1982): 279-291.
• Shetty, Dinesh K., Alan R. Rosenfield, and Winston H. Duckworth. "Mixed-mode fracture in biaxial stress state: application of the diametral-compression (Brazilian disk) test." Engineering Fracture Mechanics 26.6 (1987): 825-840.
• Nakano, M., et al. "Dynamic fracture initiation in brittle materials under combined mode I/II loading." Le Journal de Physique IV 4.C8 (1994): C8-695.
• Awaji, Hideo, and Sennosuke Sato. "Combined mode fracture toughness measurement by the disk test." Journal of Engineering Materials and Technology 100.2 (1978): 175-182.
• Jia, Z., A. Castro-Montero, and S. P. Shah. "Observation of mixed mode fracture with center notched disk specimens." Cement and Concrete research 26.1 (1996): 125-137.

## Slide 5
5
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Outline
Introduction
Stationary Cracks
• Dynamic Loading
• Initiation criterion
Growing Cracks – Mode I
• Asymptotic fields
• Crack tip equation of motion
• Limiting speed
• Transient effects
• Crack arrest
Shear Cracks
• Failure mode transition
• Dynamic interfacial fracture
• Intersonic crack growth
Crack faces
Crack front
Crack plane

## Slide 6
6
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Introduction – LEFM Revisited
3. The elastic solution furnishes a stress near the crack tip as:
Basic Hypotheses of LEFM
Cracks are inherently present in a material and there is a limit to the sensitivity of crack-detecting equipment
  NDI evaluation
2. A crack is a free, internal, planar surface in a linear-elastic stress field.
where, is the stress intensity factor (SIF), and are polar coordinates, is the applied stress, is the crack length, and is a constant that depends on geometry and crack opening mode.
Crack faces
Crack front
Crack plane
4. The crack growth leading to failure is predicted based on the tensile stress acting at the crack tip.
• Investigated in Lab 2

## Slide 7
7
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Introduction – LEFM Revisited
In LEFM, loads are felt simultaneously over all of the body
Body under load has a stiffness which works against the applied load, resulting in a displacement field satisfying equilibrium equations.
Westergaard
solution:
For crack initiation:
Ductile solids
Brittle solids
LEFM
Notes: Note there is no time dependence the solution

## Slide 8
8
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Introduction – Dynamic fracture
“Dynamic fracture mechanics is the subfield of fracture mechanics concerned with fracture phenomena for which the role of material inertia becomes significant”
- L. B. Freud, 1990
In dynamic fracture mechanics, loads felt by a material point are dependent on time:
– a non-equilibrium field
Wave motion and wave interactions must be accounted for to properly represent the material state.
transient crack tip fields
Material stiffness and inertial resistance to loading evolve.
Point 1
Point 2

## Slide 9
9
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Introduction – Dynamic fracture
Question: When is material inertia significant?
1) Rapid loading application
stress wave interactions with a stationary crack
strain-rate dependent material response
2) Rapid crack propagation
stress waves are emanated from a propagating crack
Rule of thumb:
Ramp
rate
Characteristic time:
Transmission time:
crack
Minimal inertia effects when,
Significant inertia effects when,
Geometry is important too.
Notes: The denominator of the characteristic time gets larger the faster the jump in the loading state.

## Slide 10
10
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Introduction
A 3-D symmetric problem: spherical cavity in an infinite body where a jump in pressure is applied. ( and
Using elasto-statics,
(elliptical equilibrium field)
Using elasto-dynamics,
(hyperbolic wave field)
Take-away: During dynamic fracture mechanics, wave interactions with the stationary (or propagating crack) can lead to stress intensity factors (SIFs) greater than the elasto-statics stress intensity factors.
Stress intensity factors become field and time dependent!!
dynamic
static

## Slide 11
11
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Outline
Introduction
Stationary Cracks
• Dynamic Loading
• Initiation criterion
Growing Cracks – Mode I
• Asymptotic fields
• Crack tip equation of motion
• Limiting speed
• Transient effects
• Crack arrest
Shear Cracks
• Failure mode transition
• Dynamic interfacial fracture
• Intersonic crack growth

## Slide 12
12
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Cracks
Fundamental Assumptions:
Small strain formulation of continuum mechanics
Cracks are planar features
In-plane fields only ( is independent of and )
Wave motion/interaction will play a role in the stresses experienced at a material point, therefore, we must revise our near crack stress field:
: time dependent elastic SIF
angular stress field variation
•
: order unity crack tip contribution
• for when a crack is traction free
Notes: K(t) is not a material property it is a description of a time dependent stress field

## Slide 13
13
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Mode I
Mode-I crack under sudden normal traction along the crack surface in an infinite LEHI body
Traction boundary conditions:
For
Symmetry conditions:
Implies,
for
Near the crack tip the stress field will be dominated, fields are homogeneous, variation in the stresses:
where, is a dimensionless constant
Notes: The stress intensity factor is known up to the value of C_I

## Slide 14
14
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Mode I
We can derive an analytical solution to determine the time history of
The Wiener-Hopf approach (Freund 1990, pg 77-93)
The normal stress on the crack plane for a material with
Dynamic solution
Singular solution
Notes: The stress intensity factor is known up to the value of C_I

## Slide 15
15
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Mode II
We can derive an analytical solution to determine the time history of
The shear stress on the crack plane for a material with
Dynamic soln
Singular soln
Shear wave arrival
Freund, 1990
Notes: The stress intensity factor is known up to the value of C_I

## Slide 16
16
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Initiation
A stationary crack,
For,
Waves are generated at each crack tip
Position plotted to the right
Freund, 1990
Rayleigh wave
Shear wave
Dilatational wave
Notes: Here L is our characteristic length

## Slide 17
17
Stationary Crack – Initiation
For a dynamic case assuming, where, is the smallest applied stress to satisfy criterion
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Penny shaped crack
Leading edge of a propagating pulse
When
• short crack
• long pulse duration
When
• long crack
• short pulse duration
Notes: Here L is our characteristic length

## Slide 18
18
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Initiation
Experimental results compared to fits of the normalized stress amplitude and pulse length to satisfy a stress intensity factor criterion.
Shockey et al, IJF, 1983
Short crack response
Long crack response
Crack growth
No-crack growth
Epoxy
Freund 1990
Notes: Here L is our characteristic length

## Slide 19
19
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Measurement of
Boundary/load displacement measurements
Strain Gauges
Optical techniques, e.g., caustics, coherent gradient sensing, Twyman-Green, Moiré
Notes: Here L is our characteristic length

## Slide 20
20
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Stationary Crack – Rate Effects
Investigation of the relationship between impact fracture toughness of PMMA and dynamic stress intensity factor
Wada et al, EFM, 1993
Notes: Here L is our characteristic length

## Slide 21
21
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Outline
Introduction
Stationary Cracks
• Dynamic Loading
• Initiation criterion
Growing Cracks – Mode I
• Asymptotic fields
• Crack tip equation of motion
• Limiting speed
• Transient effects
• Crack arrest
Shear Cracks
• Failure mode transition
• Dynamic interfacial fracture
• Intersonic crack growth

## Slide 22
22
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
Steady state mode 1 crack growth:
Stress field around the crack tip:
Notes: Here L is our characteristic length

## Slide 23
23
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
Elastodynamic particle velocity fields are also root singular:
Energy to crack tip:
Triaxiality:
for
for
Notes: Here L is our characteristic length

## Slide 24
24
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
Can visualize the principle stresses about the crack tip using different approaches.
Circumferential (Hoop) stress:
(deg.)
Observations:
When max stress occurs along the crack plane
When max stress occurs at ~60⁰ to the crack plane
Notes: Here L is our characteristic length

## Slide 25
25
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
(deg.)
Principal stress variation:
Observations:
Opening stress on the crack plane increases drastically with increasing crack propagation velocity
Maximas at 0 and 105⁰
Notes: Here L is our characteristic length

## Slide 26
26
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
(deg.)
Maximum shear stress:
Observations:
Monotonic increase in max shear stress with increasing crack speed for a fixed SIF level ()
Maximum shear stress does not lie on the crack plane
Notes: Here L is our characteristic length

## Slide 27
27
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Observation Interpretation
A brittle ceramic subjected to impact loading of increasing velocity
Takeaway: The greater the impact velocity (crack velocity) the greater the presence of crack bi-furcation
Notes: Here L is our characteristic length

## Slide 28
28
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Announcements
Due date for Lab 3 manuscripts: April 23rd through 27th
Final presentations (Groups 2 and 4) : May 1st 10:30am
Manuscript for Lab 4 will be reduced down to a technical note following the format of Engineering Fracture Mechanics.
technical notes are generally only 5 pages in print
limited to 3-4 figures (exp. set-up and results only)
Due date for all Lab 4 manuscripts: May 2nd by 5pm.
Notes: Here L is our characteristic length

## Slide 29
28
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Energy Approach
Analytical methods of fracture mechanics help to provide context of the validity of simulation results
Work of applied loads vs. for crack advance
Origins: Griffith 1920 (course website)
Brittle material: crack advances when the total potential energy of the body is equal to the surface energy of the new crack surface
Energy release rate (): the amount of energy per unit length along the crack edge supplied by the elastic energy in the body and by the loading system creating the new fracture surface
crack driving force
DERIVATION
Notes: Here L is our characteristic length

## Slide 30
29
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Asymptotic Fields
Taking the same approach ( is a rectangle), can find the general solution for the energy release rate for moving crack:
The functions, , and are universal functions, meaning they are independent of the applied loading and body geometry.
’
Notes: Here L is our characteristic length

## Slide 31
30
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Reminder: Growing Crack – Asymptotic Fields
Steady state mode 1 crack growth:
Stress field around the crack tip:
Notes: Here L is our characteristic length

## Slide 32
31
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Universal Solutions
Universal solutions have been found to allow for the scaling of equilibrium field solutions to obtain the dynamic solution.
SIF for a dynamic mode I crack:
universal function
equilibrium solution
Energy release rate for mode I crack:
Universal Solution
Notes: Here L is our characteristic length

## Slide 33
32
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Equation of Motion
From continuum mechanics we can solve field equations for the known motion of a propagating crack:
Motion of a crack edge
Body configuration
Applied loading
Mechanical fields
However, an appropriate theoretical model of dynamic crack growth, the motion of the crack should follow from analysis, not from prior knowledge.
Work around: utilize the universal solution approach!!
For brittle crack growth, can use a critical SIF approach (Irwin) or critical energy release rate approach (Griffith)
Notes: Here L is our characteristic length

## Slide 34
33
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Equation of Motion
Griffith based criterion: crack growth must occur such that the crack tip energy release rate is always equal to the dynamic fracture energy of the material
Available energy release rate
• loading and geometry dominated
Dynamic fracture toughness
• material property dominated
• measured in experiments!
From our universal solutions:
Solve for E.O.M:
• no term because crack is mass-less
• same approach for SIF is valid
Notes: Here L is our characteristic length

## Slide 35
34
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Measurement of
The method of caustics is a convenient approach to recording dynamic stress intensity factors and crack propagation velocities:
Notes: Here L is our characteristic length

## Slide 36
35
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Crack – Measurement of
Zehnder and Rosakis, 1990
Steel 4340
Meyers, 2004
Homalite (polymer)
In a wide range of materials it has been seen that the dynamic stress intensity factor increases with increasing crack velocity
material agnostic observation
Notes: Here L is our characteristic length

## Slide 37
36
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Cracks – “Limiting Speed”
To maintain a non-zero energy release rate, we need
Theoretical limit:
Heuristic argument: At the material offers zero resistance to growth
Most experimental observations find,
Crack branching occurs due to the Hoop stress maximum being at positions above and below the crack plane (slide 24).
Notes: Here L is our characteristic length

## Slide 38
37
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Growing Cracks – “Limiting Speed”
Question: What if we attempt to suppress crack branching by purposely integrating a week plane, coincidental to the crack plane?
Washabaugh and Knauss, IJF, 1994
“Rehealed” PMMA interface
Capacitor bank loading
As the healing strength decreases, the crack propagation velocity increases to the Rayleigh wave speed
Notes: Here L is our characteristic length

## Slide 39
38
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Outline
Introduction
Stationary Cracks
• Dynamic Loading
• Initiation criterion
Growing Cracks – Mode I
• Asymptotic fields
• Crack tip equation of motion
• Limiting speed
• Transient effects
• Crack arrest
Shear Cracks
• Mixed Mode Initiation
• Failure mode transition
• Experimental Techniques

## Slide 40
39
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Mixed Mode Crack Initiation
Mixed mode stress field:
Energy release rate:
Mode-II
Mode-I
Mixed mode loading can lead to crack kinking
Notes: Here L is our characteristic length

## Slide 41
a
altered crack path
40
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
How can we predict crack kinking? Maximum hoop (opening) stress criterion
Express the stress field in terms of the Hoop stress:
Define a mode mixity measure:
The kink angle is thus such that
and
Mixed Mode Crack Initiation
Notes: The kink angle found is at a local maximum

## Slide 42
41
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
For an inclined center crack problem:
“Fracture locus” for , plane:
If :
and
If :
and
Remember:
Mixed Mode Crack Initiation
Notes: Here L is our characteristic length

## Slide 43
42
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experimental results of Erdogan and Sih (course website) of an inclined crack in plexiglass
Pure mode I
Hoop stress prediction can be viewed as a lower bound estimate
Mixed Mode Crack Initiation
Notes: Here L is our characteristic length

## Slide 44
43
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Mixed Mode Crack – Alternative Criteria
Maximum Strain Energy Density (Sih 1972):
as
Crack propagates along the angle at which S() is a minimum
path requiring the least energy
Maximum Energy Release Rate (Erdogan and Sih 1973, Palinaswamy and Knauss 1974):
before
’
after
SIF after crack kinking:
values for , etc. can be found in legacy texts
Energy Release Rate:
kink angle when G() is maximized
Notes: Here L is our characteristic length

## Slide 45
44
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
Measurement of dynamic initiation fracture toughness
Goals:
1) Evaluate the rate dependence of mode I dynamic initiation fracture toughness ()
2) Construct the mixed mode fracture toughness locus for a given rate
3) Study the crack kinking angle as a function of mode mixity and determine the applicability of the maximum hoop stress criterion for crack initiation
In this experiment we will measure the dynamic crack initiation of PMMA; a brittle polymer at room temperature. The goal is to assess both the rate and mode mixity dependence of the material’s fracture toughness. Mode mixity will be introduced using a pre-cracked Brazil disc specimen geometry in diametral compression. Dynamic values of will be obtained using a SPHB for different projectile impact velocities. Quasi-static values of will be determined from provided data on the course website. Because a load-drop indicative of fracture may not be easily identifiable in they dynamic data, a conductive paint gauge and electrical circuit will be used to measure crack initiation.
Once the rate sensitivity of has been established, the dependence of dynamic fracture toughness on mode mixity will be evaluated. Mixed mode dynamic experiments will be conducted by inclining the Brazil disk in the SHPB so that the crack is at an angle to the diametral loading. This will allow variation of mixity from pure mode I to almost pure mode II. In the same fashion as before (i.e., using the static results), and will be measured as a function of mode mixity for one particular rate. Having extracted the values of fracture toughness, the maximum opening (hoop) stress criterion can be used to calculate the predicted angle of crack initiation. The analytical results can be then compared to the experimentally observed kinking angles.

## Slide 46
45
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
1) Evaluate the rate dependence of mode I dynamic initiation fracture toughness ()
Goals:
Select three (3) increasing striker bar impact velocities
0.5 in/min
0.05 in/min
0.005 in/min
Data on course website
Specimen failure
Trans. signal

## Slide 47
46
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
2) Construct the mixed mode fracture toughness locus for a given rate
Goals:
For the same gas gun pressure, select 6 inclinations to investigate
Note: normalize by quasi static fracture toughness values

## Slide 48
47
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
3) Study the crack kinking angle as a function of mode mixity and determine the applicability of the maximum hoop stress criterion for crack initiation
Goal:
Hint: search for M.A. Meggiolaro, 2005 EFM

## Slide 49
48
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experiment Four
References:
• Atkinson, C., R. E. Smelser, and Jo Sanchez. "Combined mode fracture via the cracked Brazilian disk test." International Journal of Fracture 18.4 (1982): 279-291.
• Shetty, Dinesh K., Alan R. Rosenfield, and Winston H. Duckworth. "Mixed-mode fracture in biaxial stress state: application of the diametral-compression (Brazilian disk) test." Engineering Fracture Mechanics 26.6 (1987): 825-840.
• Nakano, M., et al. "Dynamic fracture initiation in brittle materials under combined mode I/II loading." Le Journal de Physique IV 4.C8 (1994): C8-695.
• Awaji, Hideo, and Sennosuke Sato. "Combined mode fracture toughness measurement by the disk test." Journal of Engineering Materials and Technology 100.2 (1978): 175-182.
• Ryoji, Yuuki, et al. "Mixed mode fracture criteria for an interface crack." Engineering Fracture Mechanics 47.3 (1994): 367-377.
• Jia, Z., A. Castro-Montero, and S. P. Shah. "Observation of mixed mode fracture with center notched disk specimens." Cement and Concrete research 26.1 (1996): 125-137.

## Slide 50
49
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experimental Techniques - Thermoplasticity
During deformation there is a competition between strain, strain rate hardening and thermal softening
Strain rate hardening
Thermal softening
Thermo-mechanical
coupling
Mode 1
Stress
distance from crack tip
Crack
Plastic response
Region of dominance
(
Linear
Elastic
Notes: Here L is our characteristic length

## Slide 51
50
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Thermoplasticity
Ratio of mechanical energy converted to heat:
2. Neglect the thermo-elastic effect
• small contribution
1. Adiabatic conditions
• typical of high strain rate deformation
Simplifications:
Transient heat conduction equation:
• expresses the relationship between mechanical deformation fields and an additional unknown temperature field
: material density
: heat capacity
: fraction of mech. power converted to heat
: thermal conductivity
: coefficient of thermal expansion
: Poisson’s ratio
Notes: Here L is our characteristic length

## Slide 52
51
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Thermoplasticity
Use infrared thermography (or embedded thermocouple) to measure heat generated by dynamically growing crack (Zehnder and Rosakis, JMPS, 1991):
IR detector elements
Detector sensitivity
Notes: Here L is our characteristic length

## Slide 53
52
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experimental Techniques – Grid and Foil
Microfabricated grids
Notes: Here L is our characteristic length

## Slide 54
54
© Owen Kingstedt, 2018
ME EN 6960: Spring 2018
Experimental Techniques – Grid and Foil
Guide for creating a foil gauge:
Lightly sand specimen to create a rough surface
Bond copper terminals to the specimen surface
Apply a piece of masking tape to the surface leaving a small gap between the machined crack and the tape edge
Apply a thin layer of conductive silver paint and let dry.
Check resistivity across the conductive paint.
Notes: Here L is our characteristic length