## Slide 1
Determination of Dynamic Tensile Strength of Concrete Using a Split Hopkinson Pressure Bar
1
May 1, 2018
University of Utah
Nik Benko, John Callaway, Nick Dorsett, Martin Raming
ME EN 6960
May 1, 2018

## Slide 2
2
Concrete Failure
Introduction: Concrete Failure
Concrete is a common building material – bridges, buildings, roadways, etc.
Concrete is strong in compression and weak in tension.
Failure of concrete structures is often the result of tensile failure.
Failure of concrete is dependent on the loading rate. [1]
Design of structure needs to account for loading rate.
May 1, 2018
University of Utah

## Slide 3
3
Mechanical Testing of Concrete
Introduction: Mechanical Testing of Concrete
Tensile testing of concrete using a Brazil Disc Specimen (ASTM D 3967-08):
May 1, 2018
University of Utah
t = thickness of specimen
P
P
D
Compression creates a tensile failure of the specimen
Test can be performed quasi-statically or dynamically at high strain rates

## Slide 4
4
Split Hopkinson Pressure Bar (SHPB)
May 1, 2018
University of Utah
  In 1914, Hopkinson introduced a technique for measuring dynamic material strength
    Cylindrical steel bar with pellet lightly attached to end
    Response of bar determined by measuring momentum of pellet
  In 1948, Davies did a critical review of this experimental technique
    Microphone and oscillograph used to make photographic record
    Dispersion correction equations derived
  Kolsky further adapted Davies’ method in 1949 by introducing a second bar on the other end of the specimen with a second microphone at the end
    Record made of both incident and transmitted pulses [2]
Introduction: Split Hopkinson Pressure Bar

## Slide 5
5
Bar Setup
Introduction: Split Hopkinson Pressure Bar
Utilizes thin bars to propagate stress wave into sample
  Thin bars simplify motion into one dimension
  Bars must be homogenous and have a uniform cross section
  The impact from the striker bar must not exceed elastic limit
Strain caused by stress wave is measured at the midpoint of each bar.
  Full Wheatsone bridge configuration used to isolate axial strain
Dispersion effects present from finite bars
May 1, 2018
University of Utah

## Slide 6
6
Dispersion Correction
Methods: Dispersion Correction
Two primary methods of dispersion correction
  Pulse Shaping [3]
    Addition of a material between the incident and striker bar – lead, plastic, paper, etc.
    Creates a mechanical filter that reduces frequency content of the impulse wave(s).
    Pulse shaper material depends on SHPB and specimen materials
    Pulse shaped signal should mimic material response of specimen
May 1, 2018
University of Utah
  Post Processing [4]
    Utilize non-linear curve fitting and Fourier series to correct for dispersion

## Slide 7
7
Wave Position Correction
Methods: Wave Position Correction
Since strain gauges are positioned in the middle of the incident and transmitted bars, waves must be transmitted forward/backwards in time.
Utilizing the bar wave speed and known position of strain gauges – waves are aligned in time.
Force equilibrium can then be determined by converting voltages to strain.
May 1, 2018
University of Utah
Incident Wave
Transmitted Wave
Reflected Wave

## Slide 8
8
Test Procedures
Methods: Test Procedure
Gas gun was utilized to propel striker bar, pressure was varied from 8 to 12.5 psi.
Concrete Brazil Disc specimens were 19.05 mm in diameter and 6.35 mm thick.
SHPB were made of 7075-T6 aluminum.
Lead pulse shaper was 9.525 mm in diameter and 1.058 mm thick.
Sampling was at 125 MHz with a period of 1ms.
May 1, 2018
University of Utah

## Slide 9
9
Dynamic Tensile Strength
Results: Dynamic Tensile Strength
Dynamic Tensile Strength:
Mean: 15.77 MPa; Median: 15.18 MPa Standard Deviation: 3.60 MPa
May 1, 2018
University of Utah
Weibull Analysis:
Where:
xo = 7.84 MPa
b = 17.18 MPa
m = 4.9951

## Slide 10
10
Gas Gun Pressure and Tensile Strength
[1] Reference Text Size
Results: Gas Gun Pressure
Gas Gun Pressure and Strain Rate were expected to be correlated.
No correlation was seen when looking at cumulative class data.
May 1, 2018
University of Utah

## Slide 11
11
Conclusions
[1] Reference Text Size
Conclusion
A positive correlation between strain rate and ultimate tensile strength was confirmed
  Minimal to no correlation between gas gun pressure and strain rate
Weibull statistical analysis performed on data
  Moderate variance in strength values
Further investigation of strain rate using a measured striker bar velocity would allow the relationship between strain rate and tensile strength to be better quantified
May 1, 2018
University of Utah

## Slide 12
12
Acknowledgements
[1] Reference Text Size
Acknowledgements
Dr Owen Kingstedt and the High Strain-Rate Mechanics of Materials Laboratory for use of testing equipment and laboratory facilities
May 1, 2018
University of Utah

## Slide 13
13
References
[1] Reference Text Size
References
[1] X. Jin, C. Hou, X. Fan, C. Lu, H. Yang, X. Shu, and Z. Wang, \Quasi-static and dynamic experimental studies on the tensile strength and failure pattern of concrete and mortar discs," in Scientic Reports, 2017.
[2] H. Kolsky, “An investigation of the mechanical properties of materials at very high stain rates of loadin,” Proc. Royal Soc., 1949.
[3] D. Frew, M. J. Forrestal, and W. Chen, \Pulse shaping techniques for testing brittle materials with a split hopkinson pressure bar," Experimantal Mechincs, vol. 42, pp. 93{106, 2002.
[4] P. Follansbee and C. Frantz, \Wave propagation in the split hopkinson pressure bar," Tansactions of the ASME, vol. 105, pp. 93{106, 1983.
May 1, 2018
University of Utah